## Slide 1: Study of glass properties as electrod for RPC
Prafulla Kumar Behera
(K. Raveendrababua, Jafar Sadiqa, B. Satyanarayana@TIFR)
aIIT Madras, India,
The XIII workshop on Resistive Plate Chambers and Related Detectors (RPC2016)
Ghent University, Belgium
25th February, 2016

## Slide 2
Prafulla Kumar Behera, IIT Madras
Introduction
Motivation
Studies
  Elemental composition
  Density measurements
  Electrical properties
  Summary
RPC performance studies
Conclusions
Outline
RPC2016 workshop@UGent

## Slide 3: Motivation
The India-based Neutrino Observatory (INO) collaboration is planning to build a 50 kton magnetized Iron Calorimeter (ICAL).
The main aims of the ICAL experiment is to precisely measure the θ13 , θ23 and to determine the ordering of neutrino masses that are involved in the atmospheric neutrino oscillations.
The layout of three modular form of INO-ICAL detector.
Prafulla Kumar Behera, IIT Madras
RPC2016 workshop@UGent

## Slide 4: Motivation
The active elements in the INO-ICAL detector are glass RPCs of 2 m x 2 m in area and are 28,800 in number
There is a need of rigorous studies on the glass samples for the better selection of RPC electrodes
Resistive Plate Chamber (RPC)
A detailed characterization studies on the glass samples from various manufacturers, viz. Asahi, Italian, Japanese and Saint-Gobain, have been performed
Prafulla Kumar Behera, IIT Madras
RPC2016 workshop@UGent

## Slide 5: Elemental Composition Study
Element | Asahi (%) |  |  | Italian (%) |  |  | Japanese (%) |  |  | Saint-Gobain (%) |  |  | Variation (%)
 | Area-1 | Area-2 | Average | Area-1 | Area-2 | Average | Area-1 | Area-2 | Average | Area-1 | Area-2 | Average | 
Silicon (Si) | 15.43 | 16.69 | 16.06 | 17.56 | 16.85 | 17.21 | 16.6 | 16.86 | 16.73 | 17.24 | 17.69 | 17.47 | 1.44
Oxygen (O) | 70.93 | 68.65 | 69.79 | 68.76 | 69.81 | 69.29 | 71.06 | 70.38 | 70.72 | 71.03 | 70.65 | 70.84 | 1.55
Sodium (Na) | 10.46 | 10.71 | 10.59 | 10.33 | 10.02 | 10.18 | 9.18 | 9.26 | 9.22 | 8.70 | 8.21 | 8.46 | 2.13
Magnesium (Mg) | 2.21 | 2.51 | 2.36 | 2.13 | 2.21 | 2.17 | 2.21 | 2.34 | 2.28 | 1.64 | 2.19 | 1.92 | 0.44
Calcium (Ca) | 0.96 | 1.38 | 1.17 | 1.18 | 1.08 | 1.13 | 0.91 | 1.12 | 1.02 | 1.39 | 1.26 | 1.33 | 0.31
Iron (Fe) | 0.02 | 0.05 | 0.035 | 0.05 | 0.04 | 0.045 | 0.04 | 0.04 | 0.04 | 0.00 | 0.00 | 0.00 | 0.045
Measured using FEI Quanta 200 Scanning Elemental Microscope (SEM) and from Energy-dispersive X-ray Spectroscopy (EDS) technique.
Variation in composition is less than 3%
Prafulla Kumar Behera, IIT Madras
RPC2016 workshop@UGent

## Slide 6: Density Measurement
The density of the glass samples were measured using METTLER-AE163 laboratory weighing balance, which works on the Archimedes buoyancy principle. The pure water is used as reference fluid.
Volume of the sunken object = Volume of the displaced fluid
ρ = (W1/W2) ρ0,
W1 = Weight of the object in air,
W2 = (Weight of object in air – Apparent weight of object in water),
ρ0 = density of water at 27.40C
(room temperature) = 0.996676 g/cc.
Prafulla Kumar Behera, IIT Madras
RPC2016 workshop@UGent

## Slide 7
Density Measurement
Manufacturer | Sample number | W1 (g) | W2 (g) | Density (g/cc) | Average density (g/cc)
Asahi | 1 | 0.8958 | 0.357 | 2.5 | 2.4996
 | 2 | 0.9464 | 0.3757 | 2.51 | 
 | 3 | 0.8232 | 0.3296 | 2.489 | 
Italian | 1 | 0.5186 | 0.3148 | 1.6418 | 1.6467
 | 2 | 0.5685 | 0.3464 | 1.6356 | 
 | 3 | 0.5801 | 0.3477 | 1.6627 | 
Japanese | 1 | 0.4414 | 0.1744 | 2.5224 | 2.5029
 | 2 | 0.4052 | 0.1597 | 2.5286 | 
 | 3 | 0.4212 | 0.1708 | 2.4577 | 
Saint-Gobain | 1 | 0.705 | 0.2814 | 2.4968 | 2.4963
 | 2 | 1.0387 | 0.4162 | 2.4872 | 
 | 3 | 0.8144 | 0.324 | 2.505 | 
Italian glass density is ~ 50 % lower than others
Prafulla Kumar Behera, IIT Madras
RPC2016 workshop@UGent

## Slide 8: Relative Permittivity
In ideal conditions, most of the applied voltage should be dropped across the gas gap. From the continuity of electric filed displacement at the electrode/gas interface
D = εp Ep = εg Eg .
Where, εp and εg are the relative permittivities, and Ep and Eg are the electric fields for the electrode plate and the gas gap, respectively.
The bigger the inequality of εp> εg, the voltage drop across the gas gap.
Prafulla Kumar Behera, IIT Madras
RPC2016 workshop@UGent

## Slide 9: Relative Permeability Conti…
The relative permittivity of the glass samples was measured using “Novocontrol Broadband Dielectric/Impedance Spectrometer” at 200C.
Saint-Gobain glass sample is having the lowest relative permittivity values among the four glass samples.
The RPCs made of electrodes with larger relative permittivity
values can be operated at lower bias voltages.
Prafulla Kumar Behera, IIT Madras
RPC2016 workshop@UGent

## Slide 10: Summary
Variation in composition is less than 3%
Italian glass density is ~ 50 % lower than others
Saint-Gobain glass sample is having the lowest relative permittivity values among the four glass samples.
Prafulla Kumar Behera, IIT Madras
RPC2016 workshop@UGent

## Slide 11: RPC Performance Studies
The 2 mm gap glass RPCs of 30 cm X 30 cm size were made from Asahi and Saint-Gobain manufacturers. The thickness of electrodes is 3 mm.
The outer surfaces of the electrodes were coated with specially made graphite paint, which facilitates applying high voltage across the electrodes.
The electrodes were separated using polycarbonate spacers having a bulk resistivity ~ 1012 Ω-cm.
The conductive pickup-strips are orthogonally mounted on the external surfaces of the gap.
A layer of mylar insulator separates the electrodes and the pickup-strips.
Prafulla Kumar Behera, IIT Madras
RPC2016 workshop@UGent

## Slide 12: Gas flow system
A gas mixture of HFC-R134a/iso-C4H10/SF6 = 95/4.5/0.5 was flown through the RPCs using polyurethane tubes and the detectors were operated in avalanche mode.
Detector is operated at flow rate of 10 SCCM
Prafulla Kumar Behera, IIT Madras
RPC2016 workshop@UGent

## Slide 13: Experimental Set up
A common telescope was set up with three plastic scintillation counters to get a 3-fold coincidence. The dimensions of the scintillation counters are:
Scintillation counter position | Dimension (Length X Width X Thickness)
Top | 30 cm X 2 cm x 1 cm
Middle | 30 cm x 3 cm x 1 cm
Bottom | 30 cm x 5 cm x 1 cm
Prafulla Kumar Behera, IIT Madras
RPC2016 workshop@UGent
Notes: Insert a photo

## Slide 14: Results
Higher value of relative permittivity implies the better insulator and that implies the less leakage current. Hence, RPCs made of Asahi glass electrodes show comparatively low values of leakage current than the Saint-Gobain RPCs.
Prafulla Kumar Behera, IIT Madras
RPC2016 workshop@UGent

## Slide 15: Detector Efficiency
The knee of efficiency plateaus of Asahi RPCs started from 10.7 kV, Saint-Gobain RPCs started from 12 kV.
Prafulla Kumar Behera, IIT Madras
RPC2016 workshop@UGent

## Slide 16: Conclusions
The RPC electrode properties were studied in detail. The glass samples from four of the manufacturers shown the identical elemental composition.
The density of Italian glass sample is about two-thirds of that of the other three samples.
Saint-Gobain glass sample is having the lowest relative permittivity values among the four glass samples.
RPCs are made with the glass electrodes from Asahi and Saint-Gobain manufacturers. Asahi glass RPCs could be operated at about 1 kV lower bias voltages than Saint-Gobain glass RPCs.
Prafulla Kumar Behera, IIT Madras
RPC2016 workshop@UGent

## Slide 17: Ageing studies of glass RPC in avalanche mode operation
The effect of water vapor on the performance of glass RPC in avalanche mode operation.
It was observed significant degradation in the performance of RPC with wet gas flow.
Investigations are made to understand the causes of degradation.
Charge collected per an event
Time resolution
Wet gas
Wet gas
Dry gas
Dry gas
New Glass
Anode
Cathode
RPC2016 workshop@UGent
Prafulla Kumar Behera, IIT Madras

## Slide 18: Thank You
Dr. Prafulla Kumar Behera, IIT Madras