## Slide 1: Seeing Ultrasound through Mechanoluminescence
Simon Michels
Mathias Kersemans, Philippe F. Smet, Nicolas Lammens, Joris Degrieck and Wim Van Paepegem
Simon.Michels@UGent.be Philippe.Smet@UGent.be
1
1
2
2

## Slide 2: Content
What is luminescence?
Mechanoluminescence and ultrasound
Visualization of an US radiation field
Seeing (Ultra-)Sound through Mechanoluminescence

## Slide 3: What is luminescence?
Terminology depends on the means of excitation
Common term for a luminescent material: “Phosphor”
Seeing (Ultra-)Sound through Mechanoluminescence

## Slide 4
Ba0.98Si2O2N2:Eu0.02 : Emission spectrum
Seeing (Ultra-)Sound through Mechanoluminescence
What is luminecence?
λem = 312 nm
2+

## Slide 5
Ba0.98Si2O2N2:Eu0.02 : Excitation spectrum
Seeing (Ultra-)Sound through Mechanoluminescence
What is luminecence?
2+

## Slide 6
Ba0.98Si2O2N2:Eu0.02
Seeing (Ultra-)Sound through Mechanoluminescence
What is luminecence?
λem = 312 nm
2+

## Slide 7
Persistent luminescence: afterglow at RT
Mechanism: traps in the host material
What is luminecence?
Seeing (Ultra-)Sound through Mechanoluminescence

## Slide 8
Persistent luminescence: afterglow at RT
Mechanism: traps in the host material
What is luminecence?
Seeing (Ultra-)Sound through Mechanoluminescence

## Slide 9
Persistent luminescence: afterglow at RT
Mechanism: traps in the host material
What is luminecence?
Seeing (Ultra-)Sound through Mechanoluminescence

## Slide 10
Persistent luminescence: afterglow at RT
Mechanism: traps in the host material
What is luminecence?
Seeing (Ultra-)Sound through Mechanoluminescence
Detrapping by phonon absorption
with probability:
ΔE

## Slide 11: Mechanoluminescence and ultrasound
ML: Sudden and intense emission after mechanical stimulation (most often an increase in afterglow)
Destructive ML: fracturing
Non-destructive ML: piezoelectric host crystal
Piezoluminescence, Elasticoluminescence
Seeing (Ultra-)Sound through Mechanoluminescence

## Slide 12: Mechanoluminescence and ultrasound
ML: Sudden and intense emission after mechanical stimulation (most often an increase in afterglow)
Destructive ML: fracturing
Non-destructive ML: piezoelectric host crystal
Piezoluminescence, Elasticoluminescence
Seeing (Ultra-)Sound through Mechanoluminescence

## Slide 13: Mechanoluminescence and ultrasound
Piezoelectrically induced electron detrapping model
Seeing (Ultra-)Sound through Mechanoluminescence

## Slide 14: Mechanoluminescence and ultrasound
Piezoelectrically induced electron detrapping model
Non-centrosymmetric unit cell
Seeing (Ultra-)Sound through Mechanoluminescence

## Slide 15: Mechanoluminescence and ultrasound
In this work:
Mechanical stimulation through ultrasound
Acoustically induced
Piezo-
Luminescence
Seeing (Ultra-)Sound through Mechanoluminescence

## Slide 16
Ultrasound: longitudinal pressure wave in a medium
with f > 20 kHz
Alternating compression and rarefaction: continuous ML stimulation
Mechanoluminescence and ultrasound
Seeing (Ultra-)Sound through Mechanoluminescence
Image from Physics of Musical Sounds, John Askill. D. Van Nostrand Company (1979)

## Slide 17: 3D-reconstruction of US radiation
1 min of UV charging, integration between 450 and 550 nm
Seeing (Ultra-)Sound through Mechanoluminescence

## Slide 18
Relative Increase (RI) and Area (A)
Seeing (Ultra-)Sound through Mechanoluminescence
3D-reconstruction of US radiation

## Slide 19
Numerical simulation using FFT-BPM
Seeing (Ultra-)Sound through Mechanoluminescence
Mathias Kersemans et al. Fast Reconstruction of a Bounded Ultrasonic Beam
using Acoustically induced Piezo-Luminescence. Apl. Phys. Let. 107, 234102 (2015)

## Slide 20
Experimental setup: detection in reflection
Seeing (Ultra-)Sound through Mechanoluminescence
Mathias Kersemans et al. Fast Reconstruction of a Bounded Ultrasonic Beam
using Acoustically induced Piezo-Luminescence. Apl. Phys. Let. 107, 234102 (2015)

## Slide 21
Seeing (Ultra-)Sound through Mechanoluminescence
Mathias Kersemans et al. Fast Reconstruction of a Bounded Ultrasonic Beam
using Acoustically induced Piezo-Luminescence. Apl. Phys. Let. 107, 234102 (2015)

## Slide 22
Seeing (Ultra-)Sound through Mechanoluminescence
Mathias Kersemans et al. Fast Reconstruction of a Bounded Ultrasonic Beam
using Acoustically induced Piezo-Luminescence. Apl. Phys. Let. 107, 234102 (2015)

## Slide 23
Medical transducer with f = 3.3 MHz and I = 2.0 W/cm²
Scans with conventional hydrophone
Seeing (Ultra-)Sound through Mechanoluminescence
Mathias Kersemans et al. Fast Reconstruction of a Bounded Ultrasonic Beam
using Acoustically induced Piezo-Luminescence. Apl. Phys. Let. 107, 234102 (2015)

## Slide 24
  Near-Field Far-Field
Computed
Hydrophone
APL
Seeing (Ultra-)Sound through Mechanoluminescence
Mathias Kersemans et al. Fast Reconstruction of a Bounded Ultrasonic Beam
using Acoustically induced Piezo-Luminescence. Apl. Phys. Let. 107, 234102 (2015)

## Slide 25
Experimental setup: detection in transmission
              semi-transparent sample
Seeing (Ultra-)Sound through Mechanoluminescence
3D-reconstruction of US radiation

## Slide 26
Seeing (Ultra-)Sound through Mechanoluminescence
3D-reconstruction of US radiation

## Slide 27
Seeing (Ultra-)Sound through Mechanoluminescence
3D-reconstruction of US radiation

## Slide 28: Conclusion
Much faster/cheaper than conventional scanning
    Similair spatial resolution, can be improved
    Further automatisation of the setup
Phosphors: much room for improvement
      Short afterglow
      High APL peak intensity
      High relative increase
Seeing (Ultra-)Sound through Mechanoluminescence

## Slide 29: Thank you for your attention