## Slide 1: Heat-transfer method-based cell culture quality assay through cell detection by surface imprinted polymers
Kasper Eersels, Bart van Grinsven, Mehran Khorshid, Veerle Somers, Thomas Cleij, Ronald Thoelen, Patrick Wagner

## Slide 2: Surface Imprinting?
Sediment cells on a home-made silicone stamp (PDMS)
Spin coating removes excess buffer solution and target cells form a monolayer on the stamp
Hayden, O. and Dickert, F.L. Adv. Mater. 2001, 13, 1480-1483.

## Slide 3: Surface Imprinting?
Spin coating of a semi-cured PU layer onto aluminum substrate
Stamping of the cells in the PU layer, curing the layer overnight at 65°C
Removal of the stamp and cells creates a SIP layer imprinted for target cell type
PU: polyurethane

## Slide 4: SIP Surface Characterization
Optical microscopy
Atomic Force Microscopy
K. Eersels, B. van Grinsven et al. ACS AMI 2013, 5(15), 7258-7267.

## Slide 5: Read-Out: the Heat-Transfer Method
Rth
B. van Grinsven et al. ACS Nano 2012, 6(3), 2712-2721.
SIP

## Slide 6: Read-Out: the Heat-Transfer Method
Microcavities form preferential heat channels
Cell binding causes an increase in thermal resistance (Nakano et al.)
Heat is forced to transfer over thicker, non-imprinted region
Measured as a decrease in T2  Increase in Rth
K. Eersels, B. van Grinsven et al. ACS AMI 2013, 5(15), 7258-7267.

## Slide 7: Detection of Circulating Tumor Cells?
K. Eersels, B. van Grinsven et al. ACS AMI 2013, 5(15), 7258-7267.
Selective discrimination between tumor cells and healthy cells
Sensitivity limits applicability in CTC detection
 Improve sensitivity and find other applications

## Slide 8: Experiment
RWTH Aachen: problem with ZR-75-1 cells, grow pattern changed
STR DNA profile: over-passaging led to cross-contamination with a faster growing cell line
Reproduce circumstances: grow both cell lines for 3 months and about 25 passages in the same lab
Analyze ZR-75-1 cells with SIP-based assay on HTM

## Slide 9: Results
At passage number 15 “something” happens
Effect increases with passage number
At passage 22 Rth minimum reached
 STR DNA profile: cross-contamination!

## Slide 10: Conclusions
State-of-the-art devices (FACS) or assays (STR DNA profile) too slow and expensive for routine screening
HTM can offer a low-cost and fast alternative
Sensitivity is sufficient
Limited to changes at the membrane
Setup needs to be tested for other cell lines

## Slide 11: The end? Questions?