## Slide 1: Optical gain in 2D solution processable CdSe nanoplatelets
Belgian Physical Society Meeting
18th May 2016
Ghent, Belgium
Presented by
Renu Tomar
Ph.D Student
Physics and Chemistry of Nanostructures
(Supervisor: Prof. Zeger Hens)
Ghent University, Belgium

## Slide 2: Colloidal Quantum Dots
Colloidal quantum dots are nanometer sized (2 to 10nm) semiconductor crystallites obtained by solution-based synthesis.
Advantages:
Cheap and up-scalable synthesis
Size tunable optical properties
Shape tunable optical properties

## Slide 3: Energy level Diagram
CdSe Platelets ≈ Quantum well

## Slide 4: CdSe Platelets Synthesis
140-250 °C
140-250 °C
N2
N2
CdSe Platelets
And Cd(Ac)2
Cadmium precursor: Cadmium Acetate and Cadmium myristate in ODE
Selenium precursor: TOP-Se or ODE-Se

## Slide 5: Characterization of CdSe Platelets
TEM images of CdSe 5MLs platelets
Heavy hole (HH)
Light hole (LH)

## Slide 6: Pump-Probe Spectroscopy
ΔA<0: Bleach,reduced absorption due to state filling
ΔA>0: Photoinduced absorption,due to intraband absorption
ΔA>0 or <0: Photo-­‐induced absorptioon/bleach,due to spectral shifts
ΔA(t,λ)=A(t,λ)–A0(λ)

## Slide 7: Interaction of light with colloidal QDs
Absorption
Intraband Absorption
Stimulated emission
Auger recombination
Intraband relaxation
Multi-exciton Generation

## Slide 8: Motivation

## Slide 9
Nanoplatelets Advantages : large optical cross section, slow auger recombination rates and narrow emission linewidth
Gain in Nanoplatelets: Two different exciton density regiem
Lateral Size-Dependent Spontaneous and Stimulated Emission Properties in Colloidal CdSe Nanoplatelets (Hilmi Volkan Demir et.al. ACS Nano, 2015, 9, 5, 5041)
Continuous-wave biexciton lasing at room temperature using solution-processed quantum wells (Iwan Moreels et. al. Nature Nanotechnology, 2014, 9, 891)
Amplified Spontaneous Emission and Lasing in Colloidal Nanoplatelets (Hilmi Volkan Demir et. al. ACS Nano, 2014, 8, 7, 6599)
Single or biexciton regime
Carrier Cooling in Colloidal Quantum Wells (Dmitri V. Talapin et. al. Nano Letter. 2012, 12, 6158)
Multiexciton (~ 40 exciton per platelet)

## Slide 10: Transient Absorption Study on 4MLs CdSe Platelets
Non-linear absorption
∆A
A = A0 + ∆A
The white contour line indicates transparency () Gain is observed inside these contour
Spectra after photo-excitation with 400 nm with Pump power: 32.5 mW

## Slide 11: Characterization of CdSe Platelets
spectra, taken at 2.5 ps after photo-excitation for different pump fluences.

## Slide 12: Characterization of CdSe Platelets
Retain the excitonic feature
Gain observed in both Heavy hole (HH) and Light hole (LH)
spectra, taken 2.5 ps after photo-excitation for different pump fluences.

## Slide 13: Intrinsic absorption and <N> Calculation
Achtstein, A. W., Antanovich, A., Prudnikau, A., Scott, R., Woggon, U., Artemyev, M., J. Phys. Chem. C 2015, 119, 20156−20161
Intrinsic absorption, μi(ω) =δ (1) (ω)/VP ,
Where VP being the platelet volume and δ(1) the linear absorption cross section
… 2
… 1
… 3
Number of excitons per platelet, <N> = Jp* σ pump
Where Absorption crossection of platelets, σ pump = μi(pump) * VP
And Pump fluence, Jp = Pump power* Frequency/ (E pump* Area of pump beam)
μi(400) = 1.466 * 105 cm-1

## Slide 14: The wavelength dependent gain threshold
LH
HH
Gain threshold is 160 excitons for HH at 521 nm.
Gain threshold is 239 excitons for LH at 500 nm.

## Slide 15: Allowed optical transitions
Se - Sh
Px e - Px h

## Slide 16: Characterization of CdSe Platelets
Bleach with increase in pump power
Similar decay rate for lower pump power till onset of gain
Faster decay with increase for higher pump fluence

## Slide 17: Conclusions
  Four different monolayer thick CdSe platelets has been synthesized.
  Surface area analysis form TEM images.
  Observed gain in 4MLs Platelets in multi exciton regime.
  Need of model other than quantum-dot like models to interpret the optical properties of CdSe nanoplatelets.

## Slide 18: Thank you for your kind attention

## Slide 19: Pump-Probe Spectroscopy
ND Filter
Half Wave Plate
Chopper
500 Hz
Delay Stage
Cuvette
Non-linear
Crystal
Pump
110 fs
800nm
110 fs
Broadband Probe
Fiber to CCD

## Slide 20: The wavelength dependent gain threshold
Wavelength dependence of bleach around Heavy hole (HH) bleach wavelength.
Wavelength dependence of bleach around Light hole (LH) bleach wavelength.