## Slide 1: Thermal and Plasma-Enhanced Atomic Layer Deposition on Powders and Particles
Geert Rampelberg, Véronique Cremers, Delphine Longrie, Davy Deduytsche, Johan Haemers, Christophe Detavernier
Belgian Physical Society
General Scientific Meeting 2016
CoCooN
Conformal Coating of Nanomaterials

## Slide 2: Outline
Atomic layer deposition
Industrial applications
ALD on powders and particles
Conclusions

## Slide 3: Outline
Atomic layer deposition
  What is ALD?
  Plasma-enhanced ALD
  Advantages and limitations
  Examples of conformal nanocoatings by ALD
Industrial applications
ALD on powders and particles
Conclusions

## Slide 4: Atomic layer deposition
Gas-phase thin film deposition technique
Cyclic process of self-limiting surface reactions  layer-by-layer growth
Example : ALD growth of Al2O3 from trimethyl aluminum (TMA) and H2O
TMA pulse
Self-saturated
chemisorption
One layer of Al2O3
H2O pulse

## Slide 5: Plasma-enhanced atomic layer deposition
Plasma: Highly energetic plasma species facilitate surface reactions
More coating materials available
Coating of temperature-sensitive substrates
Cheaper chemicals
...
TMA pulse
Self-saturated
chemisorption
One layer of Al2O3
O2 plasma

## Slide 6: Advantages and limitations
Advantages:
Excellent control of thickness
Growth rate from linear fit:
0.85Å/cycle

## Slide 7: Advantages and limitations
Advantages:
Excellent control of thickness
Stoichiometry determined by chemistry
Limitations:
Slow: ~1Å/cycle
2 Al(CH3)3 + 3 H2O  Al2O3 + 6 CH4

## Slide 8: Advantages and limitations
Sol-gel
PVD
CVD
ALD
Advantages:
Excellent control of thickness
Stoichiometry determined by chemistry
Excellent uniformity
Highest degree of conformality

## Slide 9: Advantages and limitations
Advantages:
Excellent control of thickness
Stoichiometry determined by chemistry
Excellent uniformity
Highest degree of conformality
Limitations:
Slow: ~1Å/cycle
ALD = ideal technique for 3D surface engineering
Growth rate from linear fit:
0.85Å/cycle

## Slide 10: Al2O3 coated paper
ALD coated tissue paper
Thermal ALD, TMA + H2O, 50°C, 200 cycles.

## Slide 11: Al2O3 coated paper
After combustion of the cellulose template: hollow structure, consisting of freestanding 20nm Al2O3 ALD film.
Direct, macroscopic illustration of the conformality of ALD, and of its potential for coating porous and fibrous materials.

## Slide 12: ALD – a coating technique for the nano era
TiO2/V2O5/TiO2 multilayer coating of a carbon nanotube
CNT
V2O5
TiO2
TEM imaging by EMAT (UA)

## Slide 13: Outline
Atomic layer deposition
Industrial applications
  Microelectronics
  Solar energy
  Flexible electronics
ALD on powders and particles
Conclusions

## Slide 14: Functional nanocoatings in micro-electronics
Panasonic
JACS 2008, 131 (10), 3478
DRAM
Transistors
Patterning

## Slide 15: Surface passivation in photovoltaics
Batch ALD (Beneq):
2000 wafers/hour
Spatial ALD (SolayTec, Levitech):
4500 wafers/hour
Increased efficiency by enhanced lifetime of charge carriers
Dedicated reactor design

## Slide 16: Roll-to-roll ALD
Beneq: 400,000m²/year (20nm Al2O3)
Development of roll-to-roll ALD for ALD on flexible substrates
Potential use in flexible electronics

## Slide 17: Outline
Atomic layer deposition
Industrial applications
ALD on powders and particles
  UGent rotary reactor
  Applications
Conclusions

## Slide 18: Powder coater at UGent
Rotary reactor for powder agitation during gas-solid reactions
First plasma-enhanced ALD powder coater
In-situ characterization of reaction chemistry and saturation:
  Mass spectroscopy
  Optical emission spectroscopy

## Slide 19: ALD coatings on a wide range of particle sizes
Both thermal and plasma enhanced ALD can be performed on a broad range of particle sizes:
Nano ZnO
Stainless
steel
Ti
Glass beads
D. Longrie et al., Surface & Coatings Technology, 213, 183-191, 2012.

## Slide 20: Conformal Al2O3 coating on nano ZnO powder
Nano ZnO: 20-120nm particle size, 33.2 m²/g
C
O
Zn
Al
Nanopowders often form micron-sized aggregates, however, ALD is capable of conformally coating the individual nanoparticles
5nm Al2O3
D. Longrie et al., Surface & Coatings Technology, 213, 183-191, 2012.

## Slide 21: Surface functionalization of powders
Protective coatings
Moisture/oxidation:
phosphors, copper,...
Aggressive chemicals:
batteries
UV radiation:
inks, paint,...
Particle-particle interaction
Sintering:
3D printing,...
Rheology:
3D printing, pharmaceutics,...
Active functionalities
Optical coatings
Catalysts
Conductive coatings
Particle-matrix interaction
Adhesion:
fiber reinforcement ,...
Dispersion:
inks, paint,...
Hydrophobicity:
e.g. Teflon
CoCooN experience

## Slide 22: Surface functionalization of powders
Protective coatings
Moisture/oxidation:
phosphors, copper,...
Aggressive chemicals:
batteries
UV radiation:
inks, paint,...
Particle-particle interaction
Sintering:
3D printing,...
Rheology:
3D printing, pharmaceutics,...
Active functionalities
Optical coatings
Catalysts
Conductive coatings
Particle-matrix interaction
Adhesion:
fiber reinforcement ,...
Dispersion:
inks, paint,...
Hydrophobicity:
e.g. Teflon
Phosphors for LED lighting
Long term stability by encapsulation
Uncoated
10nm Al2O3
20nm Al2O3
Avci et al., J. Electrochem. Soc., 156, J333, 2009.

## Slide 23: Surface functionalization of powders
Protective coatings
Moisture/oxidation:
phosphors, copper,...
Aggressive chemicals:
batteries
UV radiation:
inks, paint,...
Particle-particle interaction
Sintering:
3D printing,...
Rheology:
3D printing, pharmaceutics,...
Active functionalities
Optical coatings
Catalysts
Conductive coatings
Particle-matrix interaction
Adhesion:
fiber reinforcement ,...
Dispersion:
inks, paint,...
Hydrophobicity:
e.g. Teflon
Batteries for Electrical Vehicles
5x longer lasting
5x faster charging
High-temperature performance
Source: Pneumaticoat
70% capacity fade after 10 years
Current Li-ion
Life cycle
Energy density
ALD coated particles
(LiNiMnOx)

## Slide 24: Surface functionalization of powders
Protective coatings
Moisture/oxidation:
phosphors, copper,...
Aggressive chemicals:
batteries
UV radiation:
inks, paint,...
Particle-particle interaction
Sintering:
3D printing,...
Rheology:
3D printing, pharmaceutics,...
Active functionalities
Optical coatings
Catalysts
Conductive coatings
Particle-matrix interaction
Adhesion:
fiber reinforcement ,...
Dispersion:
inks, paint,...
Hydrophobicity:
e.g. Teflon
Hydrophilic coating on Teflon
Coating of Teflon (hydrophobic) with ceramic coating (Al2O3, TiO2,...) results in hydrophilic behavior
Requirement of plasma-enhanced ALD!
water
droplet
Untreated Teflon: hydrophobic
Hydrophilic coating
water easily penetrates

## Slide 25: Outline
Atomic layer deposition
Industrial applications
ALD on powders and particles
Conclusions

## Slide 26: Conclusions
Atomic layer deposition:
  3D surface engineering by conformal nanocoatings
  Industrially applied in microelectronics, photovoltaics, roll-to-roll
Plasma-enhanced ALD:
  Highly energetic plasma species allow for lower deposition temperatures, wider range of coatings,...
ALD / PE-ALD on powders and particles enabled by rotary reactor:
  Nanopowders to millimeter-sized particles
  New range of applications: battery, catalysts, LED lighting,...

## Slide 27: Acknowledgements
Research Foundation Flanders
CoCooN
Conformal Coating of Nanomaterials

## Slide 28: THANK YOU