## Slide 1
Imprinting superconducting vortex footsteps in a magnetic layer
Jérémy Brisbois
Laboratory of Physics of Nanostructured Materials, ULg

## Slide 2
What is superconductivity?
Perfect conductivity
Perfect diamagnetism

## Slide 3
Conditions of existence
Magnetic field
Electric current
Tc
Hc
Jc
Superconductivity survives only under particular conditions.
H
superconductor
Temperature
Screening currents

## Slide 4
Superconducting flux vortices
Superconducting vortices are quantized unit of magnetic flux with a normal state core ~ 100 nm.
increased

## Slide 5
Flux penetration in superconductors
Smooth
flux penetration
Flux avalanches
observed by magneto-optical imaging (MOI)
vortex motion
H increased
dissipation in normal core
efficient heat removal
T raises locally

## Slide 6
Why study avalanches?
Avalanches are harmful to superconductivity and practical applications.
→ observe, control and avoid flux avalanches.
The system undergoes a dramatic transition to a state of lower energy.
T can largely rise over Tc, even over the melting point of the material.
vavalanches ~ 100 km/s

## Slide 7
Imprinting magnetic fields
Idea: use a magnetic layer to record the vortex trajectories.

## Slide 8
Sample design
Tc = 9 K
Avalanches reach the Py at full speed and at different angles.

## Slide 9
Magnetic field of the Py layer
The direction of the magnetization is easily controlled…
… and easily reversed!
In-plane saturation field ~ 2 mT

## Slide 10
Vortex footprints in the Py layer
The reversal of the in-plane magnetization leaves a head-to-head domain wall with out-of-plane field.
Before
After

## Slide 11
Imprinting flux avalanches
Printings are stable, even up to room temperature!
Guiding along the direction of magnetization
Before
After

## Slide 12
Room temperature printings
Imprinting works also at room temperature
→ tune the magnetic landscape at will
Chessboard
Printing

## Slide 13
Conclusions
Avalanches are guided by the Py layer.
The flux penetration (smooth and avalanches) can be imprinted in a magnetic layer.
The printings are stable and can even be observed at room temperature.
Perspectives:
Improve the magnetic recording of flux penetration
Tune the magnetic landscape at will to guide avalanches

## Slide 14
Thank you for your attention!

## Slide 15
M
Vortex footprints in the Py layer II
Before
After

## Slide 16
Magneto-optical imaging