## Slide 1: Controlling the CO adsorption on Pt clusters by dopant induced electronic structure modification
Piero Ferrari,[a] Luis M. Molina,[b] Vladimir E. Kaydashev,[a] Julio A. Alonso,[b] Peter Lievens,[a] and Ewald Janssens[a]
[a] Laboratory of Solid State Physics and Magnetism, KU Leuven, Belgium [b] Department of Theoretical, Atomic and Optical Physics, Universidad de Valladolid, Spain
BPS meeting 2016

## Slide 2
Motivation
M. M. Kimberly, J. Ind. Eng. Chem. 2004, 10, 1063.
Pt particles widely used as reaction catalysts
Problem: CO poisoning effect of Pt
DMFC performance
Time
J. Baschuk, and X. Li, Int. J. Energy Res. 2001, 25, 695.
Direct Methanol Fuel Cell

## Slide 3
Solution: Pt alloys, Pt–X (X = Sn, Ru, Mo, Nb, W, Ag, Ni)
S. Ehteshamia and S. Chan, Electrochim. Acta 2003, 93, 334.
OH groups adsorbed on X interact with CO on Pt forming CO2 and H2
Y. Ishikawa et al., Surf. Sci. 2002, 513, 98.
Alteration of the local Pt electronic structure upon alloying
Bifunctional mechanism
Electronic effect
?
N. Dimakis et al., J. Phys. Chem. C 2009, 113, 18730

## Slide 4
Cluster
CO
Reaction cell
Needle
valve
No other functional groups present in UHV → Bifunctional mechanism excluded
Simultaneous measurements on bare and doped Pt clusters
Comparison of experimental results with DFT calculations
Experiment
Clusters in the gas phase

## Slide 5
Inside reaction cell
Outside reaction cell
Mass spectra of NblPtn+ clusters
X = Nb, Mo, Sn, Ag
Lower intensity of (CO)2 complexes for NbPtn-1+ compared with Ptn+
Reaction kinetics
Model

## Slide 6
Experimental data fitted with the assumed reaction mechanism
CO pressure dependence
Backward reaction coefficients
Mo or Nb doping leads to a strong increase in kD(2)
kD(2) is not significantly affected by Sn or Ag dopants
Reaction kinetics

## Slide 7
Cluster | Bader charge X | CO EB (eV)
Pt19+ | - | 2.38
Pt18Nb+ | +1.73 | 1.81
Pt18Mo+ | +1.40 | 1.83
Pt18Ag+ | +0.37 | 2.26
Pt18Sn+ | +0.95 | 2.21
Calculations with PAW method and PBE functional
Pt19+CO
NbPt18+CO
MoPt18+CO
AgPt18+CO
SnPt18+CO
DFT simulations

## Slide 8
The smaller CO binding energy on (Nb,Mo)Pt18+ is rationalized by the large dopant to Pt charge transfer
Charge analysis

## Slide 9
Conclusions
A combined mass spectrometric and DFT study showed the influence of doping on the CO interaction with small cationic Pt clusters
Sn and Ag occupy low coordinated positions in the investigated Pt clusters
The magnitude of the effect strongly depends on the dopant atom
Nb and Mo occupy highly coordinated positions concomitant with a large dopant–Pt charge transfer, affecting the local electronic structure of all Pt atoms
Current results show the importance of local electronic effects on the CO adsorption. Similar mechanisms may also be present in larger Pt-X alloy nanoparticles showing enhanced CO tolerance

## Slide 10: Thanks for your attention

## Slide 11
Statistical modelling explains why under current experimental conditions
No effect of dopant on the adsorption of the first CO molecule
Second CO molecule only adsorb on larger clusters (n > 16)
Dopant-induced decrease adsorption of (CO)2 (reaction rates) reflects reduced CO chemisorption energy, EB.
RRKM simulation